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TECHNICAL DATA – HB850R

	ITEM
	UNIT 
	PROPERTY DATA

	Structure
	-
	
[image: image2]

	Base

Thickness


	µm
	25 ± 2
ASTM D3652

	Colour
	
	RED

	Total
Thickness


	µm
	65 ± 3
ASTM D3652

	Peel
Strength


	gf/25mm
	750 ± 100
ASTM D3330

	Tensile Strength
	kg/25mm
	25 ~ 28
ASTM D3759

	Elongation
	%
	110 ~ 130
ASTM D3759

	Breakdown Voltage
	kv 
	5

ASTM D149

	Temperature Use Range
	-
	-50˚C ~ 180˚C  Long Term
>200˚C  Short Term

	Chemical Resistance
	-
	Good
(20% HCI, NaOH / 20hrs)


 - Silicone Adhesive


 - Primer








 - PET Film








The data given herewith represent average values and should not be taken to write technical specifications. They are put forward in good faith but are not guaranteed. In particular the Customer should satisfy themselves of the suitability of the product for its intended use.

Storage should be in a dry well ventilated room in their initial packaging with a reasonable constant temperature around 20oC.

The product should always be applied to clean,dry surfaces. 

