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PPI SP-2125 LEAD FOIL PRESSURE SENSITIVE TAPE
Rev.2.   03.05.07  JG

DESCRIPTION:
PPI SP-2125 IS BASED ON LEAD FOIL COATED WITH AN ACRYLIC ADHESIVE. THE LEAD FOIL PROVIDES A PROTECTION (E.G. DURING ELECTROPLATING OR RADIATION EXPOSURE) WHILE THE SYNTHETIC RESIN ADHESIVE ALLOWS EASE OF REMOVABILITY. SP-2125 IS SUPPLIED ON A RELEASE COATED POLYPROPYLENE INTERLINER.

APPLICATION:
ELECTROPLATING/RADIATION PROTECTION TAPE.

PHYSICAL PROPERTIES:                     *EN VALUE:         **ASTM VALUE:        TEST METHOD:

BASE MATERIAL:                                     LEAD FOIL

FOIL THICKNESS:                                    0.125MM                 4.9 MIL                   BS 3924

TOTAL THICKNESS:                                 0.175MM                 7.0 MIL                   BS 3924

ADHESIVE:                                             SYNTHETIC RESIN/ACRYLIC

ADHESIVE STRENGTH:                             4.9 N/CM                 36 OZ/INCH

TENSILE STRENGTH:                               35 N/CM                   20 LBS/INCH

ELONGATION:                                         12%                         12%

INTERLINER:                                          SILICONISED POLYPROPYLENE FILM 0.05MM.

* EN 60454

** ASTM D-1000























































Statements, technical information and recommendations contained herein are based on tests we believe to be reliable but they are not to be construed in any manner as warranties expressed or implied.  The user shall determine the suitability of the product for the intended use and user assumes all risk and liability whatsoever therewith.


