
EXPANDING FOAM TAPE
TECHNICAL DETAILS
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	Material:
Open-cellular polyurethane foam impregnated with a modified acrylic dispersion, no plasticizers, added flame retarding fillings. The tape has a strong self-adhesive acrylic applied to one side.
 

Density

approx. 
120 kg/m³

Colour

Black
Supplied in

Rolls pre-compressed to appr. 15-20% of original thickness

Compression resistance
DIN 53 577

appr. 4-5 kPa

Tensile strength

appr. 170 kPa

Elongation

appr. 170%

Fire resistance
DIN 4102, Teil 1

Class B1

Resistance against water penetration
DIN EN 86

600 Pa 

Air penetration
DIN EN 42

<= 0,1m³/(h*m*(daPa)n)

Temperature resistance

-40 - + 100°C 
shortly to +130°C

Acceptance to other building materials

extremely
good

Storage time

2 years

Storage temperature

20°C




Due to its fine qualities, this expanding foam sealing tape has a very wide range of application within modern building, where today’s demands on reliable sealing solutions have significantly increased over the past few years.

It is applied where demands on joint constructions are exceptional. This is the case e.g. in 

high-rise buildings, with joints experiencing major movements and in building setting special demands on resistance to exterior effects.

